## Slide 1: Fluxonium
2023-06-14 Group meeting
Amalie Paulsen

## Slide 2: Fabrication of resonator chip5 (from MSMT)
The design
10x10 chip, 200nm Al, soft baked A4 resist, spun at 4000rpm for 1 min and baked at 115C for 2 min.
Perfect develop and etch

## Slide 3: Post strip

## Slide 4: GDSpy markers

## Slide 5: GDSpy markers

## Slide 7: Measurements of res 8 6.918GHz