## Slide 1: Fluxonium
2023-08-02 Group meeting
Amalie T. J. Paulsen

## Slide 2: Josephson junctions (JJ)
Design of JJ
Varying width of JJ (100-360nm) 20 nm inbetween
Fabricated in 3 steps
Base layer
JJ layer
Patches layer

## Slide 3: Chip_8_JJ2 dose test of JJ in Quantech
Post develop
Base layer

## Slide 4: Chip_8_JJ2 dose test of JJ in Quantech
Post develop
Double angle evaporation in Plassys
JJ layer
Chalmers paper:

## Slide 5: Chip_8_JJ2 dose test of JJ in Quantech
1045
1190
100nm – 2 different doses

## Slide 6: Chip_8_JJ2 dose test of JJ in Quantech
1045
1190
360nm – 2 different doses

## Slide 7: Chip_8_JJ2 dose test of JJ in Quantech
Post develop
Milling, Al evaporation and oxygen capping in Plassys
- Problems with the Plassys..
Patches layer
360nm JJ, DF and BF

## Slide 8: Chip_8_JJ2 dose test of JJ in Quantech
Next step on Chip_8_JJ2
Before there were no junctions, now we have junctions down to 100nm
And a good dose around 1045-1190
Problems with Plassys..
Next step
  Finish the patches
  2 probe measurements (to see if they are working even though the base layer was bad
  SEM -> decide on a final dose
Test limits of the recipe by making arrays of JJ and small junctions

## Slide 9: Josephson junctions (JJ) and array of JJ (array_JJ)
Design of JJ
Varying width of JJ (40-400nm) 40 nm inbetween
Design of array_JJ
Varying # JJ in array (30-150) 420nm junctions
Design of JJ
Varying width of JJ (40-400nm)

## Slide 10: Fluxonium/Transmon
First draft:

## Slide 11: Fluxonium/Transmon
Next step Fluxonium/Transmon
Continue reading experimental papers on Fluxonium to get good parameters of E_J, E_C and E_L and if the flux
Simulate capacitance in Ansys (maybe using Qiskit metal)
  Help from Shikhar and Ksenia

## Slide 12: Wafer_Al300nm
Design

## Slide 13: Wafer_Al300nm
Post development

## Slide 14: Wafer_Al300nm
Next step on wafer
Help from cleanroom to dice
Find out the approx etch rate (maybe using the borders)